Texas Sodium Bentonite, Inc. 2101 N. State Hwy 118 ¦ Alpine, Texas 79830 Phone: (432) 837-4444 Email: info@texassodiumbentonite.com www.texassodiumbentonite.com

1/4" Holeplug — Product Data Sheet Sodium Bentonite Borehole Sealing Products • Natural Sodium Montmorillonite Chip Sealant Document Type: Product Data Sheet (PDS) Revision: Rev. 1.0 Date: August 2026 CAS Number: 1302-78-9 EINECS: 215-108-5 Origin: Alpine, Texas, USA

## SECTION 1 — PRODUCT DESCRIPTION

The Texas Sodium Bentonite 1/4" Holeplug is a premium, naturally-mined sodium bentonite chip engineered for reliable borehole and monitoring well sealing in environmental, geotechnical, and water well drilling applications. Sized at approximately 1/4 inch (6.35 mm) nominal granule diameter, Holeplug chips are processed from high-smectite sodium bentonite ore sourced from Texas Sodium Bentonite’s Alpine, Texas mining operations in the Trans-Pecos region of West Texas.

Upon contact with water or groundwater, the sodium bentonite chips swell rapidly and uniformly, forming a dense, impermeable annular seal within the borehole annulus. The product’s high smectite content and proven swell characteristics make it the preferred choice for professionals requiring a dependable, cost-effective, all-natural borehole sealant.

Key Differentiator — Single-Origin, Batch-Tested Quality: Sourced exclusively from TSB’s West Texas deposit, the 1/4" Holeplug offers consistent mineralogy and performance batch to batch.

## SECTION 2 — TYPICAL APPLICATIONS

Primary Applications

| • Environmental monitoring well installation and decommissioning (grouting annular space) | • Geotechnical borehole sealing and abandonment |
| --- | --- |
| • Water well annular sealing (potable and non-potable wells) | • Vadose zone and saturated zone monitoring well completion |
| • Groundwater remediation well sealing | • Soil boring abandonment per regulatory requirements (EPA, TCEQ, state agency protocols) |
| • Horizontal directional drilling (HDD) borehole sealing applications |  |

Secondary Applications

| • Waste containment barrier component | • Landfill monitoring well installation |
| --- | --- |
| • Geotechnical investigation sealing | • Underground utility bore sealing |

## SECTION 3 — MINERALOGICAL COMPOSITION

### 3.1  Bulk Mineralogical Analysis (XRD)

Source: Bulk X-Ray Diffraction (XRD) Analysis — TSB Alpine Deposit, Trans-Pecos Region, West Texas

| Mineral | % by Weight (XRD) | Notes |
| --- | --- | --- |
| Smectite (Sodium Montmorillonite) | 54.6% | Primary swelling mineral; responsible for sealing performance |
| Opal-C | 11.2% | Amorphous silica phase; minor component |
| Quartz (SiO₂) | 11.1% | Non-swelling accessory mineral |
| K-Feldspar | 8.8% | Non-swelling accessory mineral |
| Plagioclase | 5.5% | Non-swelling accessory mineral |
| Calcite | 2.8% | Minor carbonate component |
| Clinoptilolite | 2.5% | Natural zeolite; minor component |
| Muscovite | 1.7% | Minor mica phase |
| Gypsum | 1.0% | Minor sulfate phase |
| Rutile | 0.1% | Trace titanium oxide |
| Cristobalite | 0.07% | Trace amorphous silica polymorph |

### 3.2  Chemical Composition (XRF)

Source: X-Ray Fluorescence (XRF) Analysis — TSB Alpine Deposit

| Oxide | % by Weight (XRF) | Notes |
| --- | --- | --- |
| SiO₂ | 60.29% | Silica (dominant oxide) |
| Al₂O₃ | 13.04% | Alumina |
| Fe₂O₃ | 2.63% | Iron oxide |
| CaO | 2.94% | Calcium oxide |
| Na₂O | 1.79% | Sodium oxide |
| K₂O | 1.56% | Potassium oxide |
| MgO | 1.61% | Magnesium oxide |
| TiO₂ | 0.35% | Titanium oxide |
| MnO | 0.040% | Manganese oxide |
| P₂O₅ | 0.04% | Phosphorus pentoxide |
| V₂O₅ | 0.007% | Vanadium pentoxide |
| Cr₂O₃ | <0.01% | Chromium oxide (trace) |

## SECTION 4 — PHYSICAL AND PERFORMANCE SPECIFICATIONS

| Parameter | Value / Result | Test Standard / Method |
| --- | --- | --- |
| Physical Form | Natural sodium bentonite chip | — |
| Color | Light grey to whiteish-grey | — |
| Odor | Odorless | — |
| Nominal Chip Size | 1/4 inch (approx. 6.35 mm) | — |
| Moisture Content | 9.6% | ASTM D2216 |
| pH (field sample, as-tested) | 9.28 | Laboratory measurement |
| pH (5% solids suspension) | 9.0 – 10.5 | SDS reference |
| Swell Index | 14 mL / 2 g | ASTM D5890 |
| Organic Content | 4.4% | ASTM D2974 |
| Relative Density (Specific Gravity) | 2.6 g/cm³ | SDS reference |
| Bulk Density | 1.0 – 1.4 g/cm³ | SDS reference |
| Solubility in Water | <0.9 mg/L at 20°C | EU Method A.6 |
| Flammability | Non-flammable | — |
| Primary Clay Mineral | Sodium Montmorillonite (Smectite) | XRD Analysis |
| CAS Number | 1302-78-9 | — |

## SECTION 5 — PARTICLE SIZE DISTRIBUTION

| Sieve / Particle Size | Percent Finer (%) |
| --- | --- |
| #10 (2.00 mm) | 100.0% |
| #16 (1.19 mm) | 100.0% |
| #30 (0.600 mm) | 99.2% |
| #50 (0.300 mm) | 98.0% |
| #100 (0.150 mm) | 95.6% |
| #200 (0.075 mm) | 91.6% |
| 0.0332 mm | 79.0% |
| 0.0210 mm | 79.0% |
| 0.0122 mm | 75.0% |
| 0.0087 mm | 71.0% |
| 0.0062 mm | 67.1% |
| 0.0044 mm | 63.1% |
| 0.0031 mm | 59.2% |
| 0.0013 mm | 55.2% |

### 5.3  Gradation Summary

| Fraction | % by Weight |
| --- | --- |
| Gravel (Coarse + Fine) | 0.0% |
| Sand (Coarse) | 0.0% |
| Sand (Medium) | 1.3% |
| Sand (Fine) | 7.1% |
| Silt | 27.0% |
| Clay | 64.6% |

### 5.4  Grain Size Coefficients

D90 = 0.0674 mm ¦ D85 = 0.0512 mm ¦ D60 = 0.0033 mm Note: D50, D30, D15, and D10 were not determined for this sample.

## SECTION 6 — PRODUCT PERFORMANCE CHARACTERISTICS

### 6.1  Swelling Behavior

Sodium bentonite undergoes significant volumetric expansion upon hydration. The smectite (sodium montmorillonite) mineral lattice absorbs water molecules between clay platelets, expanding up to 15–18 times its dry volume in freshwater conditions. The TSB Holeplug Swell Index of 14 mL/2g (ASTM D5890) confirms active swelling capacity, producing a dense, self-healing, low-permeability plug in the borehole annulus.

Swell performance is influenced by the following factors:

- Water chemistry (fresh vs. brackish vs. saline — elevated ionic strength reduces swell)

- Confining pressure (moderate confinement enhances sealing effectiveness)

- Chip placement method (tremie pipe placement recommended in saturated zones)

### 6.2  Hydraulic Sealing Performance

When properly placed and hydrated, sodium bentonite seals achieve hydraulic conductivity values typically in the range of 1×10⁻⁸ to 1×10⁻⁹ cm/sec or less under confining pressure — meeting or exceeding regulatory requirements for annular seals in most state and federal environmental monitoring protocols.

### 6.3  pH Compatibility

The alkaline pH of TSB Holeplug (9.28 field measurement; 9.0–10.5 in suspension) is consistent with sodium bentonite products. Users should note that highly acidic or highly saline groundwater conditions may reduce swell performance. Consult a geotechnical specialist for applications in aggressive chemical environments.

## SECTION 7 — INSTALLATION GUIDELINES

### 7.1  General Placement Notes

- TSB 1/4" Holeplug chips are designed for gravity placement (free-fall tremie method) or tremie-pipe assisted placement into the borehole annular space.

- Ensure the borehole is free of debris and cuttings prior to chip placement.

- Dry / unsaturated conditions: Chips may be poured directly into the annular space. Allow adequate time for hydration from native moisture or deliberate wetting.

- Saturated conditions (water table present): Use tremie pipe to deliver chips to the bottom of the seal interval — avoid bridging by pouring in lifts and sounding after each addition.

### 7.2  Chip Bridging Prevention

- Avoid pouring chips into boreholes with more than 30 feet of standing water without tremie pipe assistance — bridging can prevent chips from reaching the target depth.

- Sound the chip column with a weighted tape or rod after each 5-foot lift to confirm chips are reaching depth.

### 7.3  Hydration Time

- Allow a minimum of 24–48 hours for full chip hydration and seal development before conducting hydraulic testing or proceeding with upper completion.

- In dry, unsaturated conditions, introduce water above the chip interval to initiate hydration if native moisture is insufficient.

### 7.4  Regulatory Compliance

TSB 1/4" Holeplug is suitable for use as an annular sealant in environmental monitoring well construction per EPA RCRA, CERCLA, ASTM D5092, and applicable state environmental agency requirements (including TCEQ in Texas). Installers should verify local requirements for annular seal material, minimum seal thickness, and documentation prior to construction.

## SECTION 8 — STORAGE AND HANDLING

### 8.1  Storage

- Store in a cool, dry location protected from moisture and rainfall — bentonite begins to hydrate on contact with water.

- Keep bags sealed until point of use.

- Shelf life: Indefinite when stored dry; product is a natural mineral with no expiration in dry storage conditions.

- Stack bags no more than recommended height per packaging guidelines.

### 8.2  Handling

- Minimize dust generation during handling — airborne bentonite dust may cause mild respiratory irritation.

- Product becomes extremely slippery when wet — use appropriate footwear and exercise caution on wet surfaces.

- Use appropriate personal protective equipment as described below.

### 8.3  PPE Summary

| Hazard | Recommended PPE |
| --- | --- |
| Dust inhalation | NIOSH-approved dust mask or N95 respirator |
| Eye irritation (airborne dust) | Safety glasses with side shields or goggles |
| Skin contact | Work gloves; standard work clothing |
| Slip hazard (wet product) | Anti-slip footwear |

## SECTION 9 — SAFETY SUMMARY

This Product Data Sheet is a summary. For complete safety information, refer to the Texas Sodium Bentonite, Inc. Safety Data Sheet (SDS), CAS 1302-78-9, Revised 2025.

Key Safety Highlights (HCS 29 CFR 1910.1200): • Not classified as hazardous under HCS (29 CFR 1910.1200) • Non-flammable; non-explosive; non-reactive • Oral LD50 >2,000 mg/kg bw (rat) — low acute toxicity • Not classified as a carcinogen by OSHA, IARC, or NTP • Contains <1% w/w respirable crystalline silica (RCS) • Not a dangerous good for transport (ADR, IMDG, ICAO/IATA, RID)

### 9.1  Occupational Exposure Limits (OEL)

| Agency | Parameter | Exposure Limit |
| --- | --- | --- |
| OSHA | Respirable dust PEL-TWA | 5 mg/m³ |
| OSHA | Total dust PEL-TWA | 15 mg/m³ |
| ACGIH | Inhalable dust TLV-TWA | 10 mg/m³ |
| NIOSH | Quartz (RCS) REL-TWA | 0.05 mg/m³ |

Emergency Contact: American Association of Poison Control Centers — (800) 222-1222   |   Company Emergency: (432) 837-4444

## SECTION 10 — REGULATORY AND ENVIRONMENTAL INFORMATION

| Regulatory Item | Status / Detail |
| --- | --- |
| CAS Number | 1302-78-9 |
| EINECS | 215-108-5 |
| REACH (EU) | Bentonite is exempted from REACH registration under Annex V.7. Not classified as hazardous. |
| RCRA (US) | Not listed as a hazardous waste. Dispose per applicable local, state, and federal regulations. Landfill disposal acceptable where permitted. |
| Aquatic Toxicity | LC50 (96h) freshwater fish: 16,000 mg/L — low aquatic hazard at typical application quantities |
| Persistence / Biodegradability | Not relevant for inorganic minerals |
| Bioaccumulation | Not relevant for inorganic minerals |

## SECTION 11 — THIRD-PARTY TESTING AND QUALITY ASSURANCE

Texas Sodium Bentonite, Inc. supports its product specifications with independent third-party laboratory testing. The performance data presented in this Product Data Sheet is derived from the following verified test reports. All reports are available from Texas Sodium Bentonite, Inc. upon request.

| Test | Standard | Laboratory | Report Number | Date |
| --- | --- | --- | --- | --- |
| Particle Size Distribution & Water Content | ASTM D2216 | TSI Laboratories (TBPE No. F-9236), Weatherford, TX | MF0070-000003-00 | July 16–18, 2025 |
| Swell Index | ASTM D5890 | TSI Laboratories, Weatherford, TX | MF0070-000003-00 | July 18, 2025 |
| Swell Index | ASTM 5890 | IDIC Laboratories, Alexanderia, Egypt | IDIC Mineral Analysis | February 26, 2026 |
| Organic Content | ASTM D2974 | TSI Laboratories, Weatherford, TX | MF0070-000003-00 | July 18, 2025 |
| Bulk XRD Mineralogical Analysis | XRD | Q Mineral Laboratory | Q Mineral Analysis | March 5, 2026 |
| XRF Chemical Analysis | XRF | Q Mineral Laboratory | Q Mineral Analysis | March 5, 2026 |

## SECTION 12 — ORDERING AND PACKAGING INFORMATION

| Detail | Information |
| --- | --- |
| Product Name | Texas Sodium Bentonite 1/4" Holeplug |
| Available Packaging | 50 lb bags ¦ Bulk super sacks (1–2 ton) ¦ Bulk truck delivery (contact for availability) |
| Minimum Order | Contact TSB for current minimum order quantity and regional availability |
| Technical Support | Contact TSB directly for application-specific guidance |

To Order or Request Technical Support: Texas Sodium Bentonite, Inc. • 2101 N. State Hwy 118 • Alpine, Texas 79830 Contact Name: Billy Cox Phone: Sales - (806) 255-0122 / Office - (432) 837-4444 ¦ Email: info@texassodiumbentonite.com Website: www.texassodiumbentonite.com

ⓘ Disclaimer The information in this Product Data Sheet is based on data believed to be reliable and is offered in good faith. It is the responsibility of the user to determine the suitability of this product for their specific application. Texas Sodium Bentonite, Inc. makes no warranty, express or implied, regarding the accuracy of the information or the fitness of the product for any particular application. Users should independently verify compliance with all applicable local, state, and federal regulations prior to product use. Specifications are subject to change without notice; contact TSB for the most current version of this document. For complete hazard and safety information, refer to the current Safety Data Sheet (SDS), CAS 1302-78-9.

Texas Sodium Bentonite, Inc. • ¼" Holeplug — Product Data Sheet • Rev. 1.0 • August 2026 • www.texassodiumbentonite.com