Product Data Sheet Rev. 1.0 ¦ August 2026 Product Data Sheet Texas Sodium Bentonite, Inc. — Alpine, Texas 12/20 Screen Granular Sodium Bentonite Sodium Bentonite Granular Products ¦ CAS No. 1302-78-9

Texas Sodium Bentonite, Inc. 2101 N. State Hwy 118, Alpine, Texas 79830 Sales - (806) 255- 0122 ¦ Office - (432) 837-4444 info@texassodiumbentonite.com www.texassodiumbentonite.com

## Section 1  —  Product Description

The Texas Sodium Bentonite 12/20 Screen Granular is a naturally-mined, precision-screened sodium bentonite granule processed to pass a #12 sieve and be retained on a #20 sieve, yielding a tightly controlled nominal granule size range of approximately 0.85–1.68 mm. The 12/20 Screen occupies the middle tier of TSB's granular product line — finer than the 6/20 Screen and coarser than the Minus-20 Powder — offering a versatile, well-controlled particle size for applications requiring a balance between placement speed and fine-grain seal density.

The 12/20 Screen Granular's tightly graded particle range makes it particularly suitable for narrower borehole annuli, direct-push monitoring point completions, and applications where controlled, uniform hydration rates are preferred. The product's 64.6% clay fraction and confirmed smectite mineralogy ensure reliable swelling performance and low-permeability seal formation.

Sourced exclusively from TSB's single-origin Alpine, Texas mining operations in the Trans-Pecos region of West Texas, the 12/20 Screen Granular carries the same high-smectite TSB Alpine mineralogy across all production batches. Third-party laboratory testing by TSI Laboratories (TBPE No. F-9236) confirms particle size distribution, Atterberg limits, and performance data for each production run.

Note on Atterberg Limits: The 12/20 Screen test report documents a Liquid Limit (LL) of 134, Plastic Limit (PL) of 214, and Plasticity Index (PI) of 179 with USCS Classification ML and AASHTO A-4(0). Users should note that the PL > LL result is an atypical laboratory condition associated with the dry granular bentonite format — the mineralogical smectite content and swell index remain the primary indicators of field swelling and sealing performance for this product.

## Section 2  —  Typical Applications

### 2.1   Primary Applications

- Environmental monitoring well annular grouting — standard and narrow-diameter boreholes

- Direct-push monitoring point completion and sealing

- Geotechnical borehole sealing and abandonment

- Water well annular sealing (potable and non-potable)

- Soil boring abandonment per TCEQ, EPA RCRA, and CERCLA requirements

- Vadose zone and saturated zone monitoring well completion

- Instrument cable duct sealing in geotechnical applications

### 2.2   Secondary Applications

- Waste containment liner systems

- Pond sealing and lagoon sealant

- Landfill monitoring well installation

- Geotechnical investigation borehole abandonment

- Secondary sealant layer in multi-stage well completions

## Section 3  —  Mineralogical Composition

### 3.1   Bulk Mineralogy (XRD Analysis)

Source: Bulk X-Ray Diffraction (XRD) Analysis — TSB Alpine Deposit. Mineralogical data is representative of the TSB Alpine deposit source shared across all TSB product grades. Particle size screening does not alter mineralogical composition.

| Mineral | % by Weight (XRD) | Notes |
| --- | --- | --- |
| Smectite (Sodium Montmorillonite) | 54.6% | Primary swelling mineral; responsible for sealing and plasticity performance |
| Opal-C | 11.2% | Amorphous silica phase; minor component |
| Quartz (SiO₂) | 11.1% | Non-swelling accessory mineral |
| K-Feldspar | 8.8% | Non-swelling accessory mineral |
| Plagioclase | 5.5% | Non-swelling accessory mineral |
| Calcite | 2.8% | Minor carbonate component |
| Clinoptilolite | 2.5% | Natural zeolite; minor component |
| Muscovite | 1.7% | Minor mica phase |
| Gypsum | 1.0% | Minor sulfate phase |
| Rutile | 0.1% | Trace titanium oxide |
| Cristobalite | 0.07% | Trace amorphous silica polymorph |

### 3.2   Chemical Composition (XRF Analysis)

Source: X-Ray Fluorescence (XRF) Analysis — TSB Alpine Deposit.

| Oxide | % by Weight | Oxide | % by Weight |
| --- | --- | --- | --- |
| SiO₂ | 60.29% | MgO | 1.61% |
| Al₂O₃ | 13.04% | TiO₂ | 0.35% |
| CaO | 2.94% | MnO | 0.040% |
| Fe₂O₃ | 2.63% | P₂O₅ | 0.04% |
| Na₂O | 1.79% | V₂O₅ | 0.007% |
| K₂O | 1.56% | Cr₂O₃ | <0.01% |

## Section 4  —  Physical and Performance Specifications

Third-party testing performed by TSI Laboratories, Inc. (TBPE No. F-9236), Victoria, TX. Test reports available upon request.

| Parameter | Value | Test Standard / Method |
| --- | --- | --- |
| Physical Form | Screened sodium bentonite granule | — |
| Color | Light grey to greenish-grey | — |
| Odor | Odorless | — |
| Nominal Size Range | Pass #12 / Retain #20 (approx. 0.85–1.68 mm) | Screen analysis |
| pH (general range) | 9.0 – 10.5 | SDS reference |
| Liquid Limit (LL) | 134 | ASTM D4318 |
| Plastic Limit (PL) | 214 (see Sec. 1 note) | ASTM D4318 |
| Plasticity Index (PI) | 179 | ASTM D4318 |
| USCS Classification | ML | ASTM D2487 |
| AASHTO Classification | A-4(0) | AASHTO M 145 |
| D₅₀ (grain size) | 0.0750 mm | ASTM D422 (hydrometer) |
| D₈₅ (grain size) | 0.0502 mm | ASTM D422 |
| D₮₀ (grain size) | 0.0033 mm | ASTM D422 |
| Relative Density (Specific Gravity) | 2.6 g/cm³ | SDS reference |
| Bulk Density | 1.0 – 1.4 g/cm³ | SDS reference |
| Solubility in Water | <0.9 mg/L at 20°C | EU A.6 method |
| Flammability | Non-flammable | — |
| Primary Clay Mineral | Sodium Montmorillonite (Smectite) | XRD Analysis |
| CAS Number | 1302-78-9 | — |

## Section 5  —  Particle Size Distribution

### 5.1   Test Information

| Field | Detail |
| --- | --- |
| Testing Laboratory | TSI Laboratories, Inc. — Victoria, TX (TBPE No. F-9236) |
| Test Standard | ASTM D422 / ASTM D2216 |
| Sample Number | 13305 |
| Sample Location | Aqua Fria Ranch |
| Date Sampled | April 3, 2025 |
| Date Tested | April 17, 2025 |
| Tested By | S.A. |
| Checked By | Tom Paez, Lab Manager |
| Project Number | W-241039 |

### 5.2   Sieve Analysis Results

| Sieve / Size | Percent Finer (%) |
| --- | --- |
| #16 (1.19 mm) | 100.0% |
| #30 (0.600 mm) | 97.6% |
| #50 (0.300 mm) | 96.0% |
| #100 (0.150 mm) | 93.2% |
| #200 (0.075 mm) | 90.0% |
| 0.0332 mm | 79.0% |
| 0.0211 mm | 75.0% |
| 0.0122 mm | 75.0% |
| 0.0087 mm | 71.0% |
| 0.0062 mm | 67.1% |
| 0.0044 mm | 63.1% |
| 0.0031 mm | 59.2% |
| 0.0013 mm | 55.2% |

### 5.3   Gradation Summary

| Fraction | % by Weight |
| --- | --- |
| Gravel (Coarse + Fine) | 0.0% |
| Sand (Coarse) | 0.0% |
| Sand (Medium) | 3.1% |
| Sand (Fine) | 6.9% |
| Silt | 25.4% |
| Clay (<0.002 mm) | 64.6% |

### 5.4   Grain Size Coefficients

| D₅₀ | D₈₅ | D₮₀ |
| --- | --- | --- |
| 0.0750 mm | 0.0502 mm | 0.0033 mm |

## Section 6  —  Product Performance Characteristics

### 6.1   Swelling Behavior

The 12/20 Screen Granular delivers the high smectite swelling performance characteristic of TSB's Alpine deposit — with the tighter, mid-range particle size producing a more uniform hydration front compared to coarser grades. The 64.6% clay fraction reflects the concentrated smectite content available in this size cut. Upon hydration, individual granules swell and coalesce into a dense, self-sealing plug mass capable of filling borehole annular voids effectively in standard-diameter monitoring well completions.

### 6.2   Clay Fraction and Sealing Density

With 64.6% of particles in the clay-size fraction (<0.002 mm) and 90.0% passing the #200 sieve (0.075 mm), the 12/20 Screen carries a very high proportion of colloidal and sub-colloidal particles — directly corresponding to high smectite platelet concentration and superior inter-particle sealing density upon hydration.

### 6.3   Hydraulic Sealing Performance

When properly placed and hydrated under confining conditions, hydraulic conductivity values typically range from 1×10⁻⁸ to 1×10⁻⁹ cm/sec or lower — meeting or exceeding regulatory requirements for annular seals per ASTM D5092, EPA RCRA, CERCLA, and TCEQ protocols.

## Section 7  —  Installation Guidelines

### 7.1   General Placement

- Suitable for gravity (free-fall tremie), tremie-pipe assisted, and pumped slurry placement depending on borehole conditions.

- Dry / unsaturated zones: Pour directly into annular space in controlled lifts. Sound after each 5-foot lift.

- Saturated zones: Use tremie pipe to deliver granules to target depth. The finer particle range of the 12/20 Screen requires careful monitoring for bridging in boreholes with significant standing water — tremie pipe use is strongly recommended.

### 7.2   Direct-Push Completions

- The 12/20 Screen's controlled particle size is well-suited for direct-push monitoring point completions where annular space is narrow.

- Introduce via gravity with continuous sounding to confirm unobstructed placement.

### 7.3   Hydration Time

- Allow 24–48 hours minimum for full granule hydration and seal development.

- In dry conditions, add water above the seal interval to initiate hydration.

### 7.4   Regulatory Compliance

- Suitable per EPA RCRA, CERCLA, ASTM D5092, and applicable state agency requirements.

- Verify local and project-specific requirements before construction.

## Section 8  —  Storage and Handling

- Store in a cool, dry location protected from moisture. Keep bags sealed until point of use.

- Shelf life: Indefinite in dry storage — natural mineral, no expiration.

- Product becomes extremely slippery when wet. Use anti-slip footwear on wet surfaces.

- Minimize dust generation. Use dust mask, safety glasses, and gloves in dusty conditions.

### 8.1   PPE Summary

| Hazard | Recommended PPE |
| --- | --- |
| Dust inhalation | NIOSH-approved dust mask or N95 respirator |
| Eye irritation (dust) | Safety glasses with side shields or goggles |
| Skin contact | Work gloves; standard work clothing |
| Slip hazard (wet product) | Anti-slip footwear |

## Section 9  —  Safety Summary

Refer to the Texas Sodium Bentonite, Inc. Safety Data Sheet (SDS), CAS 1302-78-9, Revised 2025, for complete safety information. This Product Data Sheet is not a substitute for the SDS.

### 9.1   Key Safety Highlights

- Not classified as hazardous under HCS (29 CFR 1910.1200)

- Non-flammable; non-explosive; non-reactive

- Oral LD₅₀ >2,000 mg/kg bw (rat) — low acute toxicity

- Not classified as a carcinogen by OSHA, IARC, or NTP

- Contains <1% w/w respirable crystalline silica (RCS)

- Not a dangerous goods for transport (Not classified — ADR, IMDG, ICAO/IATA)

### 9.2   Occupational Exposure Limits (OELs)

| Agency | Parameter | Limit |
| --- | --- | --- |
| OSHA | Respirable dust PEL-TWA | 5 mg/m³ |
| OSHA | Total dust PEL-TWA | 15 mg/m³ |
| ACGIH | Inhalable dust TLV-TWA | 10 mg/m³ |
| NIOSH | Quartz (RCS) REL-TWA | 0.05 mg/m³ |

Emergency Contact: American Association of Poison Control Centers — (800) 222-1222 ¦ Company Emergency: (432) 837-4444

## Section 10  —  Regulatory and Environmental Information

| Item | Detail |
| --- | --- |
| CAS Number | 1302-78-9 |
| EINECS | 215-108-5 |
| REACH (EU) | Exempt under Annex V.7. Not classified hazardous. |
| RCRA (US) | Not a listed hazardous waste. Standard landfill disposal where permitted. |
| Aquatic Toxicity | LC₅₀ (96h) freshwater fish: 16,000 mg/L — low aquatic hazard. |
| Persistence / Biodegradability | Not relevant for inorganic minerals. |

## Section 11  —  Third-Party Testing and Quality Assurance

| Test | Standard | Laboratory | Sample No. | Date |
| --- | --- | --- | --- | --- |
| Particle Size Distribution | ASTM D422 | TSI Laboratories, Inc. (TBPE No. F-9236), Victoria, TX | 13305 | April 17, 2025 |
| Atterberg Limits (LL, PL, PI) | ASTM D4318 | TSI Laboratories, Inc. | 13305 | April 17, 2025 |
| Bulk XRD Mineralogical Analysis | XRD | Q Mineral Laboratory | TSB Alpine | March 6, 2026 |
| XRF Chemical Analysis | XRF | Q Mineral Laboratory | TSB Alpine | March 6, 2026 |

Test reports available upon request from Texas Sodium Bentonite, Inc. Contact info@texassodiumbentonite.com or call (432) 837-4444.

## Section 12  —  Ordering and Packaging Information

| Item | Detail |
| --- | --- |
| Product Name | Texas Sodium Bentonite 12/20 Screen Granular Sodium Bentonite |
| Available Packaging | 50 lb bags ¦ Bulk super sacks (1–2 ton) ¦ Bulk truck delivery (contact for availability) |
| Minimum Order | Contact TSB for current minimum order and regional availability |
| Address | 2101 N. State Hwy 118 ¦ Alpine, Texas 79830 |
| Phone | Sales – (806) 255-0122 ¦ Office - (432) 837-4444 |
| Email | info@texassodiumbentonite.com |
| Website | www.texassodiumbentonite.com |

Disclaimer The information in this Product Data Sheet is based on data believed to be reliable and is offered in good faith. It is the responsibility of the user to determine the suitability of this product for their specific application. Texas Sodium Bentonite, Inc. makes no warranty, express or implied, regarding the accuracy of the information or the fitness of the product for any particular application. Users should independently verify compliance with all applicable local, state, and federal regulations prior to product use. For complete hazard and safety information, refer to the current Safety Data Sheet (SDS), CAS 1302-78-9, Revised 2025.

Texas Sodium Bentonite, Inc. ¦ 12/20 Screen Granular — Product Data Sheet ¦ Rev. 1.0 ¦ August 2026 ¦ www.texassodiumbentonite.com