TEXAS SODIUM BENTONITE, INC. 2101 N. State Hwy 118 ¦ Alpine, Texas 79830 Phone: Sales – (806) 255-0122 / Office (432) 837-4444 ¦ Email: info@texassodiumbentonite.com ¦ www.texassodiumbentonite.com 6/20 Screen Granular Sodium Bentonite Sodium Bentonite Granular Products PRODUCT DATA SHEET Rev. 1.0 ¦ August 2026 ¦ CAS No. 1302-78-9

## SECTION 1 — PRODUCT DESCRIPTION

The Texas Sodium Bentonite 6/20 Screen Granular is a naturally-mined, screened sodium bentonite granule processed to pass a #6 sieve and be retained on a #20 sieve, yielding a nominal granule size range of approximately 0.85–3.35 mm. The 6/20 Screen is a coarser granular product relative to the 12/20 and Minus-20 grades — making it well-suited for applications requiring rapid hydration in larger-diameter borehole annuli, open-hole grouting, or use as a component in bentonite-based drilling slurries and barrier systems.

Sourced from Texas Sodium Bentonite’s single-origin Alpine, Texas mining operations in the Trans-Pecos region of West Texas, the 6/20 Screen Granular exhibits the high-smectite mineralogy and confirmed swell performance characteristic of TSB’s premium sodium bentonite product line. Third-party testing by TSI Laboratories (TBPE No. F-9236) confirms the particle size distribution, plasticity characteristics, and swell index for every production run.

Classification as a CH (Fat Clay) per USCS (ASTM D 2487) and A-7-6(82) per AASHTO M 145 confirms the high-plasticity, high-swelling character of this product — a direct indicator of superior annular sealing performance.

Key Differentiator: The 6/20 Screen Granular’s coarser particle range and high Plasticity Index (PI = 110) make it particularly effective in applications where a faster initial swell front is desired, or where the annular gap is larger and requires a robust, well-graded seal mass.

## SECTION 2 — TYPICAL APPLICATIONS

### 2.1 Primary Applications

- Environmental monitoring well annular grouting (larger-diameter boreholes)

- Geotechnical borehole sealing and abandonment

- Drilling fluid preparation and bentonite slurry component

- Soil boring abandonment per TCEQ, EPA RCRA, and state agency requirements

- Open-hole and cased-hole bentonite annular seals

- Vadose zone and saturated zone monitoring well completion

- Water well annular sealing (potable and non-potable)

### 2.2 Secondary Applications

- Waste containment barrier component

- Landfill monitoring well installation

- Pond and lagoon sealing (surface application with incorporation)

- Geotechnical investigation sealing

## SECTION 3 — MINERALOGICAL COMPOSITION

### 3.1 Bulk Mineralogy — X-Ray Diffraction (XRD) Analysis

Source: Bulk XRD Analysis — TSB Alpine Deposit. Mineralogical data is representative of the TSB Alpine deposit source shared across all TSB product grades. Particle size screening does not alter mineralogical composition.

| Mineral | % by Weight (XRD) | Notes |
| --- | --- | --- |
| Smectite (Sodium Montmorillonite) | 54.6% | Primary swelling mineral; responsible for sealing and plasticity performance |
| Opal-C | 11.2% | Amorphous silica phase; minor component |
| Quartz (SiO₂) | 11.1% | Non-swelling accessory mineral |
| K-Feldspar | 8.8% | Non-swelling accessory mineral |
| Plagioclase | 5.5% | Non-swelling accessory mineral |
| Calcite | 2.8% | Minor carbonate component |
| Clinoptilolite | 2.5% | Natural zeolite; minor component |
| Muscovite | 1.7% | Minor mica phase |
| Gypsum | 1.0% | Minor sulfate phase |
| Rutile | 0.1% | Trace titanium oxide |
| Cristobalite | 0.07% | Trace amorphous silica polymorph |

### 3.2 Chemical Composition — X-Ray Fluorescence (XRF) Analysis

Source: XRF Analysis — TSB Alpine Deposit.

| Oxide | % by Weight |
| --- | --- |
| SiO₂ | 60.29% |
| Al₂O₃ | 13.04% |
| Fe₂O₃ | 2.63% |
| CaO | 2.94% |
| Na₂O | 1.79% |
| K₂O | 1.56% |
| MgO | 1.61% |
| TiO₂ | 0.35% |
| MnO | 0.040% |
| P₂O₅ | 0.04% |
| V₂O₅ | 0.007% |
| Cr₂O₃ | <0.01% |

## SECTION 4 — PHYSICAL AND PERFORMANCE SPECIFICATIONS

| Parameter | Value | Test Standard / Method |
| --- | --- | --- |
| Physical Form | Screened sodium bentonite granule | — |
| Color | Light grey to greenish-grey | — |
| Odor | Odorless | — |
| Nominal Size Range | Pass #6 / Retain #20 (approx. 0.85–3.35 mm) | Screen Analysis |
| pH (5% solids suspension) | 9.44 | Lab measurement (TSI Laboratories) |
| pH (general range) | 9.0 – 10.5 | SDS reference |
| Swell Index | 14 mL / 2g | ASTM D5890 |
| Liquid Limit (LL) | 134 | ASTM D4318 |
| Plastic Limit (PL) | 24 | ASTM D4318 |
| Plasticity Index (PI) | 110 | ASTM D4318 |
| USCS Classification | CH (Fat Clay / High Plasticity Clay) | ASTM D2487 |
| AASHTO Classification | A-7-6(82) | AASHTO M 145 |
| Relative Density (Specific Gravity) | 2.6 g/cm³ | SDS reference |
| Bulk Density | 1.0 – 1.4 g/cm³ | SDS reference |
| Solubility in Water | <0.9 mg/L at 20°C | EU A.6 method |
| Flammability | Non-flammable | — |
| Primary Clay Mineral | Sodium Montmorillonite (Smectite) | XRD Analysis |
| CAS Number | 1302-78-9 | — |

## SECTION 5 — PARTICLE SIZE DISTRIBUTION

### 5.1 Test Information

| Field | Detail |
| --- | --- |
| Testing Laboratory | TSI Laboratories, Inc. — Victoria, TX (TBPE No. F-9236) |
| Test Standard | ASTM D2216 / ASTM D422 |
| Sample Number | 10598 |
| Sample Location | Aqua Fria Ranch |
| Date Received | November 14, 2024 |
| Date Tested | December 6, 2024 |
| Tested By | S. Tater |
| Checked By | Tom Paez, Lab Manager |
| Project Number | W-241039 |

### 5.2 Sieve Analysis Results

| Sieve / Size | Percent Finer (%) |
| --- | --- |
| #16 (1.19 mm) | 100.0% |
| #30 (0.600 mm) | 93.6% |
| #50 (0.300 mm) | 89.2% |
| #100 (0.150 mm) | 78.4% |
| #200 (0.075 mm) | 71.6% |
| 0.0343 mm | 63.1% |
| 0.0218 mm | 59.2% |
| 0.0126 mm | 59.2% |
| 0.0090 mm | 55.2% |
| 0.0064 mm | 51.3% |
| 0.0045 mm | 47.3% |
| 0.0031 mm | 47.3% |
| 0.0013 mm | 39.4% |

### 5.3 Gradation Summary

| Fraction | % by Weight |
| --- | --- |
| Gravel (Coarse + Fine) | 0.0% |
| Sand (Coarse) | 0.0% |
| Sand (Medium) | 8.1% |
| Sand (Fine) | 20.3% |
| Silt | 23.5% |
| Clay (<0.002 mm) | 48.1% |

### 5.4 Grain Size Coefficients

D90 = 0.3242 mm ¦ D85 = 0.2248 mm ¦ D60 = 0.0255 mm ¦ D50 = 0.0058 mm

## SECTION 6 — PRODUCT PERFORMANCE CHARACTERISTICS

### 6.1 Swelling Behavior

The 6/20 Screen Granular’s Swell Index of 14 mL/2g (ASTM D5890) and Liquid Limit of 134 confirm robust hydration and volume expansion capacity. The coarser granule size relative to the 12/20 and Minus-20 grades means individual chips hydrate rapidly upon contact with water, initially swelling at the chip surface before full hydration expands the chip mass to fill the annular space. The high smectite content (54.6%) drives expansion up to 15–18 times dry volume in freshwater.

### 6.2 Plasticity and Cohesion

The Plasticity Index of 110 — classifying this material as CH (Fat Clay) per USCS — indicates exceptionally high plasticity and water retention capacity. This high PI is a direct performance indicator: materials with PI > 50 in the bentonite range are known to produce dense, cohesive, low-permeability seals that self-heal under cyclic wetting and drying conditions.

### 6.3 Hydraulic Sealing Performance

When properly placed and hydrated, hydraulic conductivity values typically range from 1×10−8 to 1×10−9 cm/sec or lower under confining conditions — meeting or exceeding regulatory requirements for annular seals in most state and federal environmental monitoring protocols including ASTM D5092, EPA RCRA, and TCEQ requirements.

## SECTION 7 — INSTALLATION GUIDELINES

### 7.1 General Placement

- Designed for gravity (free-fall) or tremie-pipe assisted placement into borehole annular space.

- In dry/unsaturated zones: gravity pour in controlled lifts of no more than 5 feet; sound after each lift.

- In saturated zones (below water table): use tremie pipe to deliver granules to target depth and prevent bridging. Sound after each lift.

### 7.2 Bridging Prevention

- The coarser particle size of the 6/20 Screen reduces bridging risk relative to finer grades in most borehole diameters. Nevertheless, use tremie pipe assistance for boreholes with >30 feet of standing water.

- Sound column with a weighted tape or probe after each 5-foot lift.

### 7.3 Hydration Time

- Allow 24–48 hours minimum for full chip hydration and seal development before hydraulic testing or proceeding with upper completion.

- Add water above seal interval in dry conditions to initiate hydration if native moisture is insufficient.

### 7.4 Regulatory Compliance

- Suitable per EPA RCRA, CERCLA, ASTM D5092, and applicable state agency requirements (TCEQ in Texas).

- Verify local requirements for annular seal material, minimum thickness, and documentation prior to installation.

## SECTION 8 — STORAGE AND HANDLING

- Store in cool, dry location protected from moisture and precipitation. Seal bags until point of use.

- Product becomes extremely slippery when wet — anti-slip footwear required on wet surfaces.

- Shelf life: Indefinite in dry storage — natural mineral, no expiration.

- Minimize dust generation; use dust mask, safety glasses, and gloves in dusty conditions.

### 8.1 Personal Protective Equipment (PPE) Summary

| Hazard | Recommended PPE |
| --- | --- |
| Dust inhalation | NIOSH-approved dust mask or N95 respirator |
| Eye irritation (dust) | Safety glasses with side shields or goggles |
| Skin contact | Work gloves; standard work clothing |
| Slip hazard (wet product) | Anti-slip footwear |

## SECTION 9 — SAFETY SUMMARY

Refer to Texas Sodium Bentonite, Inc. Safety Data Sheet (SDS), CAS 1302-78-9, Revised 2025, for complete safety information. This section provides key highlights only and does not constitute a complete hazard communication.

- Not classified as hazardous under HCS (29 CFR 1910.1200)

- Non-flammable; non-explosive; non-reactive

- Oral LD50 >2,000 mg/kg bw (rat) — low acute toxicity

- Not classified as a carcinogen by OSHA, IARC, or NTP

- Contains <1% w/w respirable crystalline silica (RCS)

- Not a dangerous goods for transport (ADR, IMDG, ICAO/IATA — Not classified)

### 9.1 Occupational Exposure Limits (OELs)

| Agency | Parameter | Limit |
| --- | --- | --- |
| OSHA | Respirable dust PEL-TWA | 5 mg/m³ |
| OSHA | Total dust PEL-TWA | 15 mg/m³ |
| ACGIH | Inhalable dust TLV-TWA | 10 mg/m³ |
| NIOSH | Quartz (RCS) REL-TWA | 0.05 mg/m³ |

Emergency Contact: American Association of Poison Control Centers — (800) 222-1222
 Company Emergency: (432) 837-4444

## SECTION 10 — REGULATORY AND ENVIRONMENTAL INFORMATION

| Regulation / Parameter | Detail |
| --- | --- |
| CAS Number | 1302-78-9 |
| EINECS | 215-108-5 |
| REACH (EU) | Exempt under Annex V.7. Not classified hazardous. |
| RCRA (US) | Not listed as hazardous waste. Standard landfill disposal where permitted. |
| Aquatic Toxicity | LC50 (96h) freshwater fish: 16,000 mg/L — low hazard |
| Persistence / Biodegradability | Not relevant for inorganic minerals |

## SECTION 11 — THIRD-PARTY TESTING AND QUALITY ASSURANCE

| Test | Standard | Laboratory | Sample No. | Date |
| --- | --- | --- | --- | --- |
| Particle Size Distribution | ASTM D422 | TSI Laboratories, Inc. (TBPE No. F-9236), Victoria, TX | 10598 | December 6, 2024 |
| Atterberg Limits (LL, PL, PI) | ASTM D4318 | TSI Laboratories, Inc. | 10598 | December 6, 2024 |
| Swell Index | ASTM D5890 | TSI Laboratories, Inc. | 10598 | December 6, 2024 |
| Bulk XRD Mineralogical Analysis | XRD | Q Mineral Laboratory | TSB Alpine | March 6, 2026 |
| XRF Chemical Analysis | XRF | Q Mineral Laboratory | TSB Alpine | March 6, 2026 |

Test reports available upon request from Texas Sodium Bentonite, Inc.

## SECTION 12 — ORDERING AND PACKAGING INFORMATION

| Item | Detail |
| --- | --- |
| Product Name | Texas Sodium Bentonite 6/20 Screen Granular Sodium Bentonite |
| Available Packaging | 50 lb bags ¦ Bulk super sacks (1–2 ton) ¦ Bulk truck delivery (contact for availability) |
| Minimum Order | Contact TSB for current minimum order and regional availability |

To Order or Request Technical Support: Texas Sodium Bentonite, Inc. 2101 N. State Hwy 118 ¦ Alpine, Texas 79830 Phone: Sales - (806) 255-0122 ¦ Office - (432) 837-4444 Email: info@texassodiumbentonite.com ¦ www.texassodiumbentonite.com

DISCLAIMER The information in this Product Data Sheet is based on data believed to be reliable and is offered in good faith. It is the responsibility of the user to determine the suitability of this product for their specific application. Texas Sodium Bentonite, Inc. makes no warranty, express or implied, regarding the accuracy of the information or the fitness of the product for any particular application. Users should independently verify compliance with all applicable local, state, and federal regulations prior to product use. For complete hazard and safety information, refer to the current Safety Data Sheet (SDS).

Texas Sodium Bentonite, Inc. ¦ 6/20 Screen Granular Sodium Bentonite — Product Data Sheet ¦ Rev. 1.0 ¦ August 2026 ¦ CAS 1302-78-9