TEXAS SODIUM BENTONITE, INC. ¦ ALPINE, TEXAS ¦ SODIUM BENTONITE POWDER PRODUCTS Minus-20 Powder Modified Sodium Bentonite · 100% Passing #20 Sieve (0.85 mm) · Fine Ground Powder Grade Product Data Sheet ¦ Rev. 1.0 ¦ August 2026 ¦ CAS 1302-78-9

Product: Minus-20 Powder (Modified Bentonite) Document No.: TSB-PDS-M20-001 Revision: Rev. 1.0 Product Line: Sodium Bentonite Powder Products Date: August 2026 Document Type: Product Data Sheet

## SECTION 1  —  PRODUCT DESCRIPTION

The Texas Sodium Bentonite Minus-20 Powder is a finely processed, modified sodium bentonite powder with 100% of particles passing a #20 sieve (all particles finer than 0.85 mm). It is the finest product in TSB's granular product line — delivering the maximum available surface area per unit mass, the fastest hydration rate, and the highest dispersion capacity of all TSB granular and chip products.

Designated by TSI Laboratories, Inc. as "Minus 20 Powder — Modified Bentonite", this product has been further processed beyond standard screening to achieve a fine, well-distributed powder gradation ideal for applications requiring a pumpable, mixable, or slurry-based bentonite system. With 69.1% clay-fraction particles and a D90 of 0.1065 mm, the Minus-20 Powder achieves near-total sub-silt gradation — ensuring rapid and thorough dispersion in water-based systems.

Primary advantages of the powder format over chip/granular products include: near-instantaneous water absorption and swelling initiation, superior dispersion uniformity in mixed slurries, compatibility with grout pumping and injection systems, and maximum clay surface area exposure for adsorption and barrier applications.

Sourced from TSB's single-origin Alpine, Texas Trans-Pecos mining operation, the Minus-20 Powder shares the same high-smectite TSB Alpine mineralogy as all TSB products. All particle size distribution data is third-party verified by TSI Laboratories, Inc. (TBPE No. F-9236).

## SECTION 2  —  TYPICAL APPLICATIONS

### 2.1   Primary Applications

### Animal feed flow agent and pellet binder

- Bentonite grout mixing for monitoring well annular grouting (pump-mixed and injected)

- Slurry trench / cutoff wall construction — bentonite-water slurry preparation

- Geotechnical barrier and liner system construction

- Soil-bentonite backfill mixture preparation

- Borehole grouting via tremie pipe with pumped slurry

- Horizontal directional drilling (HDD) fluid preparation and lubrication

- Drilling mud and fluid loss control additive

### 2.2   Secondary Applications

- Environmental containment barrier systems

- Landfill cover and liner component — bentonite admixture

- Foundation grouting and underpinning

- Industrial sealant and adsorbent applications

- Pond and reservoir sealing by surface mixing/incorporation

.

## SECTION 3  —  MINERALOGICAL COMPOSITION

### 3.1   Bulk Mineralogy — X-Ray Diffraction (XRD) Analysis

Source Note: Mineralogical data is representative of the TSB Alpine deposit source shared across all TSB product grades. Powder processing does not alter mineralogical composition.

| Mineral | % by Weight (XRD) | Notes |
| --- | --- | --- |
| Smectite (Sodium Montmorillonite) | 54.6% | Primary swelling mineral; responsible for sealing, plasticity, and barrier performance |
| Opal-C | 11.2% | Amorphous silica phase; minor component |
| Quartz (SiO2) | 11.1% | Non-swelling accessory mineral |
| K-Feldspar | 8.8% | Non-swelling accessory mineral |
| Plagioclase | 5.5% | Non-swelling accessory mineral |
| Calcite | 2.8% | Minor carbonate component |
| Clinoptilolite | 2.5% | Natural zeolite; minor component |
| Muscovite | 1.7% | Minor mica phase |
| Gypsum | 1.0% | Minor sulfate phase |
| Rutile | 0.1% | Trace titanium oxide |
| Cristobalite | 0.07% | Trace amorphous silica polymorph |

### 3.2   Chemical Composition — X-Ray Fluorescence (XRF) Analysis

| Oxide | % by Weight |
| --- | --- |
| SiO2 | 60.29% |
| Al2O3 | 13.04% |
| Fe2O3 | 2.63% |
| CaO | 2.94% |
| Na2O | 1.79% |
| K2O | 1.56% |
| MgO | 1.61% |
| TiO2 | 0.35% |
| MnO | 0.040% |
| P2O5 | 0.04% |
| V2O5 | 0.007% |
| Cr2O3 | <0.01% |

## SECTION 4  —  PHYSICAL AND PERFORMANCE SPECIFICATIONS

| Parameter | Value | Test Standard / Method |
| --- | --- | --- |
| Physical Form | Fine powder; 100% passing #20 sieve | Screen analysis |
| Color | Light grey to greenish-grey | — |
| Odor | Odorless | — |
| Maximum Particle Size | 0.85 mm (100% passing #20 sieve) | Screen analysis |
| Product Designation | Minus-20 Modified Bentonite Powder | TSI Laboratories designation |
| D90 | 0.1065 mm | ASTM D422 (hydrometer) |
| D85 | 0.0429 mm | ASTM D422 |
| D60 | 0.0022 mm | ASTM D422 |
| pH (general range) | 9.0 – 10.5 | SDS reference |
| Relative Density (Specific Gravity) | 2.6 g/cm³ | SDS reference |
| Bulk Density | 1.0 – 1.4 g/cm³ | SDS reference |
| Solubility in Water | <0.9 mg/L at 20°C | EU A.6 method |
| Flammability | Non-flammable | — |
| Primary Clay Mineral | Sodium Montmorillonite (Smectite) | XRD Analysis |
| CAS Number | 1302-78-9 | — |

Note — Atterberg Limits & Swell Index: Atterberg Limits and Swell Index were not reported for this sample in the TSI Laboratories test report (L-003). Given the high clay fraction (69.1%) and smectite mineralogy consistent with all TSB Alpine products, swelling performance is expected to be consistent with or exceed the 1/4" Holeplug and 6/20 Screen grades. Contact TSB for additional performance data as it becomes available.

## SECTION 5  —  PARTICLE SIZE DISTRIBUTION

### 5.1   Test Information

| Field | Detail |
| --- | --- |
| Testing Laboratory | TSI Laboratories, Inc. — Victoria, TX (TBPE No. F-9236) |
| Test Standard | ASTM D422 (tested in accordance with ASTM test methods) |
| Sample Number / Figure | L-003 |
| Sample Location | Aqua Fria Ranch |
| Date Sampled | April 3, 2025 |
| Date Received | April 3, 2025 |
| Date Tested | May 12, 2025 |
| Tested By | S.A. |
| Checked By | Daniel Tesfai, P.E. |
| Project Number | W-241039 |

### 5.2   Sieve Analysis Results

| Sieve / Particle Size | Percent Finer (%) |
| --- | --- |
| #16 (1.19 mm) | 100.0% |
| #30 (0.600 mm) | 100.0% |
| #50 (0.300 mm) | 97.6% |
| #100 (0.150 mm) | 92.8% |
| #200 (0.075 mm) | 87.6% |
| 0.0330 mm | 82.9% |
| 0.0210 mm | 79.0% |
| 0.0121 mm | 79.0% |
| 0.0087 mm | 71.0% |
| 0.0061 mm | 71.0% |
| 0.0044 mm | 67.1% |
| 0.0030 mm | 63.1% |
| 0.0013 mm | 55.2% |

### 5.3   Gradation Summary

| Fraction | % by Weight |
| --- | --- |
| Gravel (Coarse + Fine) | 0.0% |
| Sand (Coarse) | 0.0% |
| Sand (Medium) | 0.8% |
| Sand (Fine) | 11.6% |
| Silt | 18.5% |
| Clay (<0.002 mm) | 69.1% |

### 5.4   Grain Size Coefficients

D90 = 0.1065 mm ¦ D85 = 0.0429 mm ¦ D60 = 0.0022 mm

Note: The Minus-20 Powder has the highest clay fraction (69.1%) of all TSB granular products — reflecting the concentration of colloidal smectite particles achieved through fine powder processing.

## SECTION 6  —  PRODUCT PERFORMANCE CHARACTERISTICS

### 6.1   Swelling Behavior — Powder Format Advantages

The Minus-20 Powder's fine particle size delivers rapid and thorough hydration upon contact with water. Unlike chip or granular products that hydrate progressively from the particle surface inward, powder-sized particles are small enough that full hydration occurs nearly instantaneously throughout each particle — resulting in faster slurry formation, more uniform dispersion, and immediate viscosity development in mixed systems.

When used as a dry powder incorporated into soil-bentonite mixtures or grouting systems, the Minus-20 Powder's maximum surface area per unit mass ensures complete contact with available water, maximizing swelling potential and minimizing the unhydrated core fraction common in coarser grades.

### 6.2   Clay Fraction and Colloidal Performance

At 69.1% clay-fraction particles — the highest of any TSB product — the Minus-20 Powder delivers the maximum colloidal smectite content per unit weight. This translates directly to superior viscosity development in slurry systems, higher gel strength in bentonite-water mixes, and maximum hydraulic sealing performance per kilogram of product applied.

### 6.3   Hydraulic Sealing Performance

When properly mixed and placed in grouting or slurry trench applications, hydraulic conductivity values for hydrated bentonite barriers typically range from 1×10−8 to 1×10−9 cm/sec or lower — meeting or exceeding regulatory requirements for containment barriers per EPA RCRA, CERCLA, and applicable state environmental standards.

### 6.4   Mixing Guidance

- Standard bentonite slurry: 40–60 lb of Minus-20 Powder per 100 gallons of fresh water (approx. 45–70 g/L) — adjust to achieve target viscosity and density for the specific application.

- Grout mix: Combine with water at the appropriate bentonite-to-water ratio per project specification; pump-mix using a high-shear mixer for maximum dispersion.

- Soil-bentonite admixture: Mix at 2–6% by dry weight of soil depending on target hydraulic conductivity and project specification.

- Use fresh, low-ionic-strength water whenever possible — elevated dissolved solids (particularly calcium and magnesium) reduce swelling and dispersion performance.

## SECTION 7  —  INSTALLATION GUIDELINES

### 7.1   Slurry and Grout Preparation

- Mix Minus-20 Powder with fresh water using a high-shear paddle mixer or colloidal mixer for a minimum of 5 minutes to achieve full dispersion before pumping.

- Allow mixed slurry to hydrate for a minimum of 30 minutes before placing in critical sealing applications.

- Pump using standard grout pumps compatible with fine-particle bentonite slurry (peristaltic or progressive cavity pumps recommended).

### 7.2   Grouted Annular Seals (Monitoring Wells)

- For pump-tremie grouted annular seals: mix slurry per Section 6.4, pump via tremie pipe from the bottom of the seal interval upward, withdraw tremie pipe as grout rises.

- Ensure borehole is free of cuttings and debris prior to grouting.

- Verify grout placement by monitoring return volumes and surface observation.

### 7.3   Slurry Trench and Cutoff Wall Applications

- Maintain slurry density and viscosity within project-specified ranges throughout trench construction.

- Monitor slurry levels continuously during excavation — keep slurry level above the groundwater table to maintain trench stability.

- Test slurry properties (density, viscosity, pH) at intervals specified in project QC plan.

### 7.4   Regulatory Compliance

Suitable for use per EPA RCRA, CERCLA, ASTM D5092, and applicable state agency requirements. Verify local requirements for grouting materials, mix ratios, and QC documentation prior to construction.

## SECTION 8  —  STORAGE AND HANDLING

⚠ DUST CAUTION — Enhanced Risk: Fine Powder Format The Minus-20 Powder generates significantly more airborne dust than chip or granular formats. Respiratory protection is strongly required during all handling, mixing, and application operations. Work upwind or in enclosed/wind-protected areas where possible. Product becomes extremely slippery when wet — anti-slip footwear required on all wet surfaces.

- Store in a cool, dry location in sealed bags or containers — powder format is highly susceptible to moisture absorption. Do not expose to rain or humidity.

- Shelf life: Indefinite in dry, sealed storage — natural mineral product; no expiration.

- Avoid generating airborne dust clouds — mix in enclosed or wind-protected areas where possible.

### 8.1   PPE Requirements — Powder Handling (Enhanced)

| Hazard | Recommended PPE |
| --- | --- |
| Dust inhalation — ELEVATED RISK (fine powder) | NIOSH-approved N95 respirator or higher; half-face respirator with P100 filters for continuous or heavy-exposure operations |
| Eye irritation — dust (elevated risk) | Safety goggles, sealed type; do NOT use open-sided safety glasses for powder handling |
| Skin contact | Work gloves; long sleeves; standard work clothing |
| Slip hazard (wet product) | Anti-slip footwear required on all wet surfaces |
| Wind-driven dust | Work upwind; use windbreak or enclosed mixing area |

## SECTION 9  —  SAFETY SUMMARY

Refer to the Texas Sodium Bentonite, Inc. Safety Data Sheet (SDS), CAS 1302-78-9, Revised 2025, for complete safety information. This section provides a summary only and does not replace the full SDS.

- Not classified as hazardous under HCS (29 CFR 1910.1200)

- Non-flammable; non-explosive; non-reactive

- Oral LD50 >2,000 mg/kg bw (rat) — low acute toxicity

- Not classified as a carcinogen by OSHA, IARC, or NTP

- Contains <1% w/w respirable crystalline silica (RCS)

- Not a dangerous good for transport (ADR, IMDG, ICAO/IATA — Not classified)

- Note: Fine powder format generates more airborne dust than chip products — use respiratory PPE during all handling operations

### 9.1   Occupational Exposure Limits (OELs)

| Agency | Parameter | Limit |
| --- | --- | --- |
| OSHA | Respirable dust PEL-TWA | 5 mg/m³ |
| OSHA | Total dust PEL-TWA | 15 mg/m³ |
| ACGIH | Inhalable dust TLV-TWA | 10 mg/m³ |
| NIOSH | Quartz (RCS) REL-TWA | 0.05 mg/m³ |

Emergency Contact: American Association of Poison Control Centers — (800) 222-1222  |  Company Emergency: (432) 837-4444

## SECTION 10  —  REGULATORY AND ENVIRONMENTAL INFORMATION

| Regulatory Framework | Status / Classification |
| --- | --- |
| CAS Number / EINECS | CAS 1302-78-9 ¦ EINECS 215-108-5 |
| REACH (EU) | Exempt under Annex V.7. Not classified as hazardous. |
| RCRA (US) | Not a listed hazardous waste. Standard landfill disposal where permitted. |
| Aquatic Toxicity | LC50 (96h) freshwater fish: 16,000 mg/L — low aquatic hazard at typical application volumes |
| Persistence / Biodegradability | Not relevant for inorganic minerals |
| Bioaccumulation | Not relevant for inorganic minerals |

## SECTION 11  —  THIRD-PARTY TESTING AND QUALITY ASSURANCE

| Test | Standard | Laboratory | Sample Reference | Date |
| --- | --- | --- | --- | --- |
| Particle Size Distribution | ASTM D422 | TSI Laboratories, Inc. (TBPE No. F-9236), Victoria, TX | L-003 | May 12, 2025 |
| Bulk XRD Mineralogical Analysis | XRD | Independent Mineralogy Laboratory | TSB Alpine | On file |
| XRF Chemical Analysis | XRF | Independent Laboratory | TSB Alpine | On file |

Test reports are available upon request from Texas Sodium Bentonite, Inc.

## SECTION 12  —  ORDERING AND PACKAGING INFORMATION

| Detail | Information |
| --- | --- |
| Product Name | Texas Sodium Bentonite Minus-20 Powder (Modified Bentonite) |
| Available Packaging | 50 lb bags; bulk super sacks (1–2 ton); bulk truck delivery (contact for availability) |
| Minimum Order | Contact TSB for current minimum order quantities and regional availability |

To Order or Request Technical Support: Texas Sodium Bentonite, Inc. 2101 N. State Hwy 118 ¦ Alpine, Texas 79830 Phone: Sales - (806) 255-0122 ¦ Office - (432) 837-4444 Email: info@texassodiumbentonite.com ¦ ww.texassodiumbentonite.com

Disclaimer The information in this Product Data Sheet is based on data believed to be reliable and is offered in good faith. It is the responsibility of the user to determine the suitability of this product for their specific application. Texas Sodium Bentonite, Inc. makes no warranty, express or implied, regarding the accuracy of the information or the fitness of the product for any particular application. Users should independently verify compliance with all applicable local, state, and federal regulations prior to product use. For complete hazard and safety information, refer to the current Safety Data Sheet (SDS), CAS 1302-78-9.

| Texas Sodium Bentonite, Inc. ¦ 2101 N. State Hwy 118, Alpine, Texas 79830 ¦ (432) 837-4444 | Minus-20 Powder — Product Data Sheet | Rev. 1.0 ¦ August 2026 |
| --- | --- | --- |