| Texas Sodium Bentonite, Inc. ¦ 2101 N. State Hwy 118, Alpine, Texas 79830 ¦ (432) 837 - 4444 ¦ info@texassodiumbentonite.com ¦ www.texassodiumbentonite.com | August 2026 ¦ Rev. 1.0 |
| --- | --- |

Sodium Bentonite Product Line — Comparison Reference Sheet

| Parameter | 1/4” Holeplug ~6.35 mm chip | 6/20 Screen Granular Pass #6 / Retain #20 | 12/20 Screen Granular Pass #12 / Retain #20 | Minus-20 Powder 100% passing #20 |
| --- | --- | --- | --- | --- |
| Product Identification |  |  |  |  |
| Product Format | Chip — borehole seal | Granule — coarse screen | Granule — fine screen | Powder — mixed/pumped |
| Nominal Size / Cut | ~6.35 mm chip (1/4 inch) | Pass #6 / Retain #20 (0.85–3.35 mm) | Pass #12 / Retain #20 (0.85–1.68 mm) | 100% passing #20 (<0.85 mm) |
| CAS Number | 1302-78-9 | 1302-78-9 | 1302-78-9 | 1302-78-9 |
| Particle Size Data — TSI Laboratories (ASTM D422) |  |  |  |  |
| TSI Sample No. | 15148 | 10598 | 13305 | L-003 |
| Test Date | July 2025 | December 2024 | April 2025 | May 2025 |
| % Passing #200 (0.075 mm) | 91.6% | 71.6% | 90.0% | 87.6% |
| % Clay Fraction (<0.002 mm) | 64.6% | 48.1% | 64.6% | 69.1% — Highest |
| % Silt Fraction | 27.0% | 23.5% | 25.4% | 18.5% |
| % Sand Fraction | 8.4% | 28.4% | 10.0% | 12.4% |
| D90 (mm) | 0.0674 | 0.3242 | 0.0750 | 0.1065 |
| D85 (mm) | 0.0512 | 0.2248 | 0.0502 | 0.0429 |
| D60 (mm) | 0.0033 | 0.0255 | 0.0033 | 0.0022 |
| Performance Data |  |  |  |  |
| pH | 9.28 (measured) | 9.44 (measured) | 9.0–10.5 (range) | 9.0–10.5 (range) |
| Swell Index (ASTM D5890) | 14 mL/2g | 14 mL/2g | 14 mL/2g | 14 mL/2g |
| Moisture Content (ASTM D2216) | 9.6% | — | — | — |
| Liquid Limit (LL) — ASTM D4318 | — | 134 | 134 | — |
| Plastic Limit (PL) — ASTM D4318 | — | 24 | 214† | — |
| Plasticity Index (PI) — ASTM D4318 | — | 110 (High) | 179 (Very High)† | — |
| USCS Classification (ASTM D2487) | — | CH — Fat Clay | ML | — |
| AASHTO Classification (M 145) | — | A-7-6(82) | A-4(0) | — |
| Organic Content (ASTM D2974) | 4.4% | — | — | — |
| Mineralogy (XRD — TSB Alpine Deposit — All Products Share Single-Origin Composition) |  |  |  |  |
| Smectite (Montmorillonite) | 54.6% | ← Same deposit — shared mineralogy across all products → | 54.6% (same) |  |
| Quartz | 11.1% | 11.1% | 11.1% | 11.1% |
| Opal-C | 11.2% | 11.2% | 11.2% | 11.2% |
| Typical Applications |  |  |  |  |
| Monitoring well annular grouting | ✓ Chip placement | ✓ Gravity or tremie | ✓ Gravity or tremie | ✓ Pump-tremie slurry |
| Borehole / boring abandonment | ✓ Primary use | ✓ | ✓ | ✓ Grout mix |
| Direct-push monitoring points | — | — | ✓ Ideal (tighter cut) | ✓ |
| Drilling fluid / slurry preparation | — | ✓ Secondary | — | ✓ Primary use |
| Slurry trench / cutoff walls | — | — | — | ✓ Primary use |
| HDD borehole sealing | ✓ | ✓ | ✓ | ✓ Fluid additive |
| Pond / reservoir sealing | — | ✓ | — | ✓ Surface mix-in |
| Placement Method |  |  |  |  |
| Gravity / free-fall placement | ✓ Preferred | ✓ Preferred | ✓ Preferred | — (requires mixing) |
| Tremie pipe placement | ✓ Recommended in saturated zones | ✓ Recommended | ✓ Recommended | ✓ Pump-tremie |
| Pump / slurry injection | — | — | — | ✓ Primary method |
| Rehydration time (minimum) | 24–48 hours | 24–48 hours | 24–48 hours | Rapid — slurry ready in 30 min |
| Storage & Packaging |  |  |  |  |
| Available formats | 50 lb bag; super sack; bulk | 50 lb bag; super sack; bulk | 50 lb bag; super sack; bulk | 50 lb bag; super sack; bulk |
| Dust generation risk | Low | Low | Moderate | HIGH — use N95 respirator |
| Shelf life (dry storage) | Indefinite | Indefinite | Indefinite | Indefinite |

† 12/20 Screen PL > LL is an atypical result associated with dry granular bentonite format. Smectite content and swell index remain primary field performance indicators.

| ◆ Single-Origin Alpine, TX Deposit — Quality Assurance All TSB products are sourced from a single-origin Alpine, Texas Trans-Pecos deposit. Single-origin sourcing ensures consistent mineralogy and smectite content batch-to-batch across all product grades. Third-party particle size, Atterberg limits, swell index, and organic content testing performed by TSI Laboratories, Inc. (TBPE No. F-9236). Full test reports available upon request. | ◆ Product Selection Guide — Which grade is right for your application? 1/4” Holeplug: Gravity chip placement in standard monitoring well annuli — self-installs, no mixing required. 6/20 Screen Granular: Coarser granule for larger-diameter holes, faster swell front, or secondary drilling fluid use. 12/20 Screen Granular: Tightly graded mid-size for narrow annuli, direct-push monitoring points, or precision grouting. Minus-20 Powder: Pumpable slurry, grout mix, slurry trench, cutoff walls, or any surface application requiring full hydration. |
| --- | --- |

| Texas Sodium Bentonite, Inc. ¦ Alpine, TX ¦ (432) 837-4444 ¦ info@texassodiumbentonite.com | Sodium Bentonite Product Line — Comparison Reference Sheet ¦ Rev. 1.0 ¦ August 2026 | For complete specifications see individual Product Data Sheets. Contact TSB for SDS. |
| --- | --- | --- |